## Slide 1: Reverse-bias stress of High Electron Mobility Transistors: correlation between leakage current, current collapse and trap characteristics
University of Padova
Department of Information Engineering

## Slide 2: Outline
Introduction
  HEMT and GaN based devices
  Trapping phenomena
Measurement Setup
Experimental Results
  Reverse bias step stress and DC characterization
  Emission Microscopy
  Current collapse
Discussion about Results
  Trap analysis (Current transient) on a fresh device
  Trap variation during stress

## Slide 3: Introduction
HEMT
High Electron mobility transistors: heterostructure composed by two layers (semiconductors with different properties).
Wide application on power conversion and communication fields: (i) maximum frequency; (ii) breakdown robustness; (iii) power dissipation
AlGaN GaN
2DEG
Ef
Ec

## Slide 4: Introduction
GaN (Gallium Nitride):
energy gap
mobility and saturation velocity
breakdown electric field
 | Si | GaAs | GaN
Eg (eV) | 1.1 | 1.42 | 3.49
µn (cm2/Vs) | 1500 | 8500 | 1000-2000
Vsat (107 cm/s) | 1 | 1.3 | 1.3
EBD (MV/cm) | 0.3 | 0.4 | 3

## Slide 5: Introduction
Trapping phenomena – Current collapse (i.e. recoverable temporary drain current reduction after the application of a high voltage)
Importance of the correlation between current collapse and gate leakage current increase due to degradation after reverse bias stress
Worsening of device performances and reliability

## Slide 6: Measurement Setup
DC characterization:
diode and transistor I-V curves
transconductance
Pulsed characterization:
custom setup
measurement bias point (VDS, VGS) pulsed from a quiescent bias point (VDSQ, VGSQ)
1µs pulse, 100 µs period
Drain current transient:
Application of a trapping and de-trapping phase (100s)
Several ambient temperature imposed (activation energy and cross section)
Light emission:
measured in OFF and ON state
Reverse bias step stress:
Bias applied for 120s
Increasing VG bias of 5V/step
light emission monitoring
Detrapping phase
300s with no bias

## Slide 7: Experimental results: Reverse bias stress
Degradation voltage: VGS=-70V, VDS=0V
Not recoverable gate leakage current increase both in diodes and transistors

## Slide 8: Experimental results: Reverse bias stress
No significant decrease after VGS=-70V, VDS=0V
Variation of main parameters partially due to trapping phenomena, partially to not recoverable degradation

## Slide 9: Experimental results: Emission Microscopy
After VGS=-70V
After VGS=-80V
EL measurements revealed hot spots after degradation voltage
Increase of hot spots and EL photon count with device degradation
Good correlation between EL measurements and transistor gate leakage current

## Slide 10: Experimental results: Trapping analysis
Four baselines applied: trap localization
I-V curves and maximum transconductance dynamic curves
(i) low voltage: no increase of gate current and current collapse
(ii) before degradation: current collapse increases but not leakage current
(iii) after degradation: strong correlation between gate leakage current and traps

## Slide 11: Discussion about results
DISCUSSION:
WHAT IS THE CAUSE OF THE CURRENT COLLAPSE INCREASE AFTER THE STRESS??
GENERATION OF NEW DEFECTIVE LEVELS?
TRAPS AMPLITUDE INCREASE?

## Slide 12: Discussion about results: Trap analysis
Two main traps
Traps are both thermal activated
Trap is identified by a variation of the current value
Peak of the dIDS/d(log10)t

## Slide 13: Discussion about results: Trap analysis
Two main traps
Traps are both thermal activated
Trap is identified by a variation of the current value
Peak of the dIDS/d(log10)t

## Slide 14: Discussion about results: Trap analysis
Two main traps with activation energy:
  T1=0.56eV
  T2=0.74eV
Comparison with literature
  T1
    Fe doping in the GaN buffer
    access region
  T2
    access region

## Slide 15: Discussion about results: Trap analysis
No variation in the activation energy or cross section (T1, T2)
No creation of new defective levels
Increase of the amplitude of both the traps
  T1: from 2.76∙10-3 to 3.52∙10-3 (28%)
  T2: from .49∙10-4 to 6.80∙10-4 (173%)